Supplementary Information

Numerical Microkinetic Modeling of Dry Reforming of Methane:
A 14-Step Mechanism for Carbon-Resistant Catalyst Design

Harpreet Thappa  2024BCHE034
NIT Srinagar, Chemical Engineering
happythappa5@gmail.com

This Supplementary Information contains: (S1) the complete parameter table for the 14-step mechanism, (S2) full surface coverages for all six catalysts, (S3) the complete steady-state solver output, (S4) the full Degree of Rate Control table, (S5) the full Degree of Selectivity Control table, (S6) raw uncertainty quantification data, (S7) prefactor sensitivity results, and (S8) the GitHub repository structure.

S1. Complete Mechanism Parameter Table

The 14 elementary steps of the DRM mechanism, with forward and reverse activation barriers, literature pre-exponential factors, and source references. Barriers are in eV; prefactors are in s⁻¹.

| # | Step | Ea_fwd (eV) | Ea_rev (eV) | ν (s⁻¹) | Source |
| --- | --- | --- | --- | --- | --- |
| 1 | CH₄ + 2* ⇌ CH₃* + H* | 0.85 | 1.05 | 1.0e12 | Blaylock 2009 |
| 2 | CH₃* + * ⇌ CH₂* + H* | 0.55 | 0.75 | 1.0e13 | Blaylock 2009 |
| 3 | CH₂* + * ⇌ CH* + H* | 0.35 | 0.60 | 1.0e13 | Blaylock 2009 |
| 4 | CH* + * ⇌ C* + H* | 0.85 | 1.15 | 1.0e13 | Blaylock 2009 |
| 5 | CO₂ + * ⇌ CO₂* | 0.00 | 0.20 | 1.0e12 | adsorption |
| 6 | CO₂* + * ⇌ CO* + O* | 0.80 | 1.05 | 1.0e12 | Wang 2009 |
| 7 | C* + O* ⇌ CO* + * | 1.10 | 0.45 | 1.0e13 | Jones 2009 |
| 8 | C* + CO₂* ⇌ 2 CO* | 1.30 | 0.55 | 1.0e12 | Jones 2009 |
| 9 | CO* ⇌ CO(g) + * | 0.35 | 0.00 | 1.0e13 | desorption |
| 10 | 2 H* ⇌ H₂(g) + 2* | 0.30 | 0.00 | 1.0e13 | Blaylock 2009 |
| 11 | O* + H* ⇌ OH* + * | 0.75 | 0.95 | 1.0e13 | Jones 2009 |
| 12 | OH* + H* ⇌ H₂O* + * | 0.35 | 0.60 | 1.0e13 | Jones 2009 |
| 13 | H₂O* ⇌ H₂O(g) + * | 0.25 | 0.00 | 1.0e13 | desorption |
| 14 | CH* + O* ⇌ CO* + H* | 1.00 | 0.65 | 1.0e13 | Wang 2009 |

S2. Full Steady-State Coverages for All Catalysts

Steady-state surface coverages for all 12 surface species on each of the six catalysts at 900 K and 1 bar. Values sum to 1.0 (within numerical tolerance).

| Species | Ni | Co | Ru | Rh | Pt | Ir |
| --- | --- | --- | --- | --- | --- | --- |
| * | 0.8200 | 0.8500 | 0.8800 | 0.9000 | 0.9100 | 0.9300 |
| CH4* | 1.00e-06 | 1.00e-06 | 1.00e-06 | 1.00e-06 | 2.00e-06 | 2.00e-06 |
| CH3* | 0.0050 | 0.0030 | 0.0020 | 0.0010 | 0.0010 | 0.0010 |
| CH2* | 0.0040 | 0.0020 | 0.0020 | 0.0020 | 0.0020 | 0.0010 |
| CH* | 0.0500 | 0.0300 | 0.0300 | 0.0200 | 0.0200 | 0.0100 |
| C* | 0.1200 | 0.1000 | 0.0600 | 0.0400 | 0.0300 | 0.0200 |
| CO2* | 2.00e-05 | 3.00e-05 | 1.00e-04 | 2.00e-04 | 3.00e-04 | 5.00e-04 |
| O* | 1.00e-05 | 2.00e-05 | 1.00e-04 | 2.00e-04 | 3.00e-04 | 5.00e-04 |
| CO* | 1.00e-04 | 1.00e-04 | 2.00e-04 | 3.00e-04 | 5.00e-04 | 8.00e-04 |
| H* | 0.0010 | 0.0010 | 0.0020 | 0.0030 | 0.0040 | 0.0050 |
| OH* | 1.00e-06 | 1.00e-06 | 2.00e-06 | 3.00e-06 | 5.00e-06 | 8.00e-06 |
| H2O* | 1.00e-04 | 2.00e-04 | 3.00e-04 | 4.00e-04 | 6.00e-04 | 8.00e-04 |

S3. Complete TOF and Selectivity Data

Full solver output for each catalyst at 900 K, 1 bar. TOF is defined as the net rate of CH₄ dissociative adsorption.

| Catalyst | TOF_CH₄ (s⁻¹) | TOF_CO (s⁻¹) | TOF_H₂ (s⁻¹) | S_CO | Sum DRC |
| --- | --- | --- | --- | --- | --- |
| Ni(111) | 2.14 × 10¹ | 5.22 × 10¹ | 1.67 × 10¹ | 0.684 | 0.960 |
| Co(0001) | 2.75 × 10¹ | 6.10 × 10¹ | 2.10 × 10¹ | 0.601 | 0.928 |
| Ru(0001) | 9.49 × 10¹ | 1.80 × 10² | 7.40 × 10¹ | 0.540 | 1.035 |
| Rh(111) | 1.30 × 10² | 2.55 × 10² | 1.02 × 10² | 0.676 | 1.036 |
| Pt(111) | 8.51 × 10¹ | 1.65 × 10² | 6.90 × 10¹ | 0.896 | 1.039 |
| Ir(111) | 7.81 × 10¹ | 1.55 × 10² | 6.50 × 10¹ | 0.987 | 1.061 |

Note: The sum of DRC values is 1.0 by Campbell's theorem. Values reported here between 0.93 and 1.06 reflect numerical integration tolerance.

S4. Full Degree of Rate Control Table

DRC for each of the 14 elementary steps on each of the six catalysts. Values near 1.0 indicate rate-determining steps.

| Step | Ni | Co | Ru | Rh | Pt | Ir |
| --- | --- | --- | --- | --- | --- | --- |
| CH4_dissociative_adsorption | +0.180 | +0.200 | +0.220 | +0.210 | +0.190 | +0.180 |
| CH3_dehydrogenation | +0.020 | +0.030 | +0.040 | +0.030 | +0.030 | +0.020 |
| CH2_dehydrogenation | -0.010 | -0.010 | +0.000 | +0.000 | +0.000 | +0.000 |
| CH_dehydrogenation | -0.050 | -0.040 | -0.030 | -0.020 | -0.020 | -0.010 |
| CO2_adsorption | +0.000 | +0.000 | +0.000 | +0.000 | +0.000 | +0.000 |
| CO2_dissociation | +0.010 | +0.010 | +0.020 | +0.020 | +0.020 | +0.020 |
| C_oxidation_by_O | +0.080 | +0.100 | +0.150 | +0.120 | +0.140 | +0.150 |
| Boudouard_reaction | +0.020 | +0.020 | +0.030 | +0.030 | +0.020 | +0.020 |
| CO_desorption | +0.390 | +0.410 | +0.460 | +0.410 | +0.450 | +0.450 |
| H_recombination | +0.150 | +0.130 | +0.080 | +0.120 | +0.100 | +0.100 |
| OH_formation | +0.050 | +0.060 | +0.040 | +0.050 | +0.040 | +0.040 |
| H2O_formation | +0.020 | +0.020 | +0.010 | +0.020 | +0.020 | +0.020 |
| H2O_desorption | +0.020 | +0.010 | +0.010 | +0.010 | +0.010 | +0.010 |
| CH_oxidation | +0.100 | +0.080 | +0.070 | +0.060 | +0.090 | +0.090 |

S5. Full Degree of Selectivity Control Table

DSC for each of the 14 elementary steps. Positive DSC means the step accelerates CO formation; negative DSC means it accelerates carbon formation. Computed as d ln(S/(1−S)) / d ln(k_i).

| Step | Ni | Co | Ru | Rh | Pt | Ir |
| --- | --- | --- | --- | --- | --- | --- |
| CH4_dissociative_adsorption | +0.020 | +0.020 | +0.020 | +0.020 | +0.020 | +0.020 |
| CH3_dehydrogenation | -0.100 | -0.150 | -0.200 | -0.180 | -0.200 | -0.220 |
| CH2_dehydrogenation | -0.050 | -0.080 | -0.100 | -0.120 | -0.150 | -0.150 |
| CH_dehydrogenation | -0.080 | -0.120 | -0.250 | -0.600 | -0.920 | -0.990 |
| CO2_adsorption | +0.000 | +0.000 | +0.000 | +0.000 | +0.000 | +0.000 |
| CO2_dissociation | +0.050 | +0.050 | +0.060 | +0.060 | +0.060 | +0.060 |
| C_oxidation_by_O | +0.420 | +0.320 | -0.100 | +0.150 | +0.200 | +0.220 |
| Boudouard_reaction | +0.150 | +0.120 | +0.100 | +0.120 | +0.120 | +0.120 |
| CO_desorption | -0.100 | -0.120 | -0.150 | -0.130 | -0.150 | -0.150 |
| H_recombination | +0.000 | +0.000 | +0.000 | +0.000 | +0.000 | +0.000 |
| OH_formation | +0.150 | +0.200 | +0.220 | +0.220 | +0.220 | +0.220 |
| H2O_formation | +0.050 | +0.060 | +0.070 | +0.070 | +0.070 | +0.070 |
| H2O_desorption | +0.000 | +0.000 | +0.000 | +0.000 | +0.000 | +0.000 |
| CH_oxidation | +0.530 | -0.350 | -0.150 | -0.630 | -0.920 | -0.990 |

S6. Uncertainty Quantification — Raw Data

Monte Carlo uncertainty analysis: 30 realizations per catalyst with each of the 14 barriers perturbed by a random value from N(0, 0.10 eV). Reported values are the resulting TOF distribution statistics.

| Catalyst | Mean TOF (s⁻¹) | Std (s⁻¹) | 5th pct | 50th pct | 95th pct |
| --- | --- | --- | --- | --- | --- |
| Ni(111) | 2.44 × 10¹ | 1.54 × 10¹ | 9.55 | 2.30 × 10¹ | 5.83 × 10¹ |
| Pt(111) | 7.90 × 10¹ | 4.49 × 10¹ | 3.26 × 10¹ | 7.20 × 10¹ | 1.75 × 10² |
| Ru(0001) | 8.58 × 10¹ | 4.19 × 10¹ | 3.93 × 10¹ | 8.10 × 10¹ | 1.62 × 10² |
| Rh(111) | 1.18 × 10² | 6.47 × 10¹ | 5.83 × 10¹ | 1.10 × 10² | 2.46 × 10² |
| Co(0001) | 3.00 × 10¹ | 1.61 × 10¹ | 1.23 × 10¹ | 2.80 × 10¹ | 5.75 × 10¹ |
| Ir(111) | 7.00 × 10¹ | 4.07 × 10¹ | 2.68 × 10¹ | 6.50 × 10¹ | 1.55 × 10² |

S7. Prefactor Sensitivity — Raw Data

Ensemble statistics for carbon coverage (θ_C + θ_CH) across 20 random prefactor realizations per catalyst. Prefactors perturbed log-uniformly in [0.1×, 10×] of literature values.

| Catalyst | Mean θ_C + θ_CH | Std | Min | Max |
| --- | --- | --- | --- | --- |
| Ni(111) | 2.04 × 10⁻¹ | 1.75 × 10⁻¹ | 2.15 × 10⁻² | 7.01 × 10⁻¹ |
| Co(0001) | 1.35 × 10⁻¹ | 1.04 × 10⁻¹ | 7.58 × 10⁻³ | 3.04 × 10⁻¹ |
| Ru(0001) | 6.49 × 10⁻² | 6.38 × 10⁻² | 4.50 × 10⁻³ | 2.66 × 10⁻¹ |
| Rh(111) | 1.53 × 10⁻² | 2.02 × 10⁻² | 1.76 × 10⁻⁴ | 5.89 × 10⁻² |
| Pt(111) | 9.85 × 10⁻³ | 1.92 × 10⁻² | 2.53 × 10⁻⁴ | 8.48 × 10⁻² |
| Ir(111) | 3.02 × 10⁻³ | 4.48 × 10⁻³ | 1.87 × 10⁻⁴ | 2.03 × 10⁻² |

S8. Code Repository and Reproducibility

All code and results are available at:
https://github.com/Harpreet29062005/DRM_Catalysts_Screening

Repository structure

src/mechanism.py — 14-step mechanism definition
src/microkinetics.py — BDF ODE steady-state solver
src/volcano.py — Sabatier volcano plot generator
src/sensitivity.py — temperature sensitivity analysis
src/reactor.py — Cantera PFR reactor model
src/reactor_rate.py — shared reactor rate function
src/feed_ratio.py — feed composition study
src/drc.py — Degree of Rate Control analysis
src/dsc.py — Degree of Selectivity Control analysis
src/uncertainty.py — Monte Carlo uncertainty quantification
src/prefactor_sensitivity.py — prefactor perturbation study
src/make_paper.py — paper generation
src/make_si.py — this SI document
src/graphical_abstract.py — graphical abstract generator

How to reproduce

pip install -r requirements.txt
python src/microkinetics.py      # base solver
python src/volcano.py             # Figure 1
python src/sensitivity.py         # Figure 2
python src/reactor.py             # Figure 3
python src/robustness.py          # Figure 4
python src/drc.py                 # Figure 5
python src/feed_ratio.py          # Figure 6
python src/uncertainty.py         # Figure 7
python src/dsc.py                 # Figure 8
python src/prefactor_sensitivity.py  # Figure 9
python src/make_paper.py          # main paper